| Typical conditions of use | Slump Range |  |
| --- | --- | --- |
|  | mm | in |
| Poured into water-free unlined bore. Widely spaced reinforcement leaving ample room for free movement between bars. | 75 to 125 | 3 to 5 |
| Where reinforcement is not spaced widely enough to give free movement between bars. Where cut-off level of concrete is within casing. Where pile diameter is less than 600mm. | 100 to 175 | 4 to 7 |
| Where concrete as placed by tremie under water or bentonite suspension | 150 to collapse | 6 to collapse |